SERS of HaCaT Genomic DNA on Ag/SiNW:
Adsorption Geometry, Frequency Shifts, and Nucleobase–Silver Interaction

DNA HaCaT 20 ng/µL on Ag/SiNW  |  532 nm, 50× LF, 0.5 s × 4 acc, 600 gr/mm  |  Maps M1–M4 (25 spectra each), n = 100  |  CaF₂ reference: 532 nm, 600 gr/mm, 10 s × 4 acc

───────────────────────────────────────────────────────────────────────────────────────────────────────────────────

1.  Introduction and Experimental

HaCaT human keratinocyte genomic DNA at 20 ng/µL, 5 µL drop-cast, was dried at room temperature. Four Raman maps (M1–M4, 25 spectra each on a 5 × 5 grid) were collected. A CaF₂ normal Raman spectrum of the same sample (532 nm, 600 gr/mm, 10 s × 4 acc) serves as a shift-free reference.  Baseline correction: airPLS (λ = 10⁵); smoothing: Savitzky–Golay (window 11, order 3); peak centres: Gaussian sub-pixel fitting (±0.1 cm⁻¹).

Figure 1.  CaF₂ Normal Raman Reference — DNA HaCaT 20 ng/µL

Figure 1.  CaF₂ normal Raman spectrum of HaCaT genomic DNA . This shift-free reference defines the unperturbed peak positions: G ring def. 667.4, A ring breathing 722.6, O-P-O/Thy+Cyt 782.7, backbone C-C/C-O 912.8, νs PO₂⁻ 1097.3, νas PO₂⁻ 1238.8, Ade+Gua 1481.0, Ade+Gua in-plane 1573.1 cm⁻¹.

2.  Results

Several spectra’s were taken , among several best spectra is plotted in reference with DNA-HaCaT on CaF2.

After acquiring several spectras, we choose best experimental conditions , 2.5%,532nm,600gr, 0.5s 4a to take a raman map across different regions. As per Professor’s advice to look deeply in to each spectra, I plotted several best spectra among 100 spectra. I also made a table for several spectra under same acquisition conditions.
When you see (m3_S20) it means map 3 spectra 20 or so on.

2.1  Cleanest Single SERS Spectrum (M3-S20, full range 200–3000 cm⁻¹)

Figure 2.  The cleanest single SERS spectrum from all 100 map spectra (M3-S20, ALS baseline-corrected, normalised). The dominant low-wavenumber feature at 242 cm⁻¹ is the Ag–N stretch confirming base-first chemisorption (Lancia et al., 2023). The Si TO phonon at 524 cm⁻¹ identifies the SiNW substrate. DNA fingerprint bands are clearly resolved at 596–1625 cm⁻¹. The silent region 1800–2900 cm⁻¹ shows a weak C≡N feature at ~2148 cm⁻¹ (Ag–CN surface complex; Bozzini et al., J. Electroanal. Chem. 563, 133, 2004) and the CH₂/CH₃ marker at ~2931 cm⁻¹ (DNA methylation; Lancia et al., 2023).

2.3  Band-by-Band Frequency Shifts (Gaussian-fitted peak centres)

Shifts Δν = ν(SERS) − ν(CaF₂). Only bands clearly resolved above noise in ≥3 maps are listed.

| Band (cm⁻¹) | CaF₂ ref | M1-S16 | M2-S20 | M3-S9 | M4-S11 |
| --- | --- | --- | --- | --- | --- |
| G ring def. 668 | 667.4 | 683.6 (+16.2) | 672.2 (+4.8) | 658.9 (−8.5) | 662.7 (−4.7) |
| A ring breath. 722 | 722.6 | 732.3 (+9.7) | 732.9 (+10.3) | 734.4 (+11.8) | 734.8 (+12.2) |
| O-P-O/Thy+Cyt 783 | 782.7 | 791.7 (+9.0) | 788.6 (+5.9) | 794.1 (+11.4) | 800.2 (+17.5) |
| Backbone C-C/C-O 912 | 912.8 | 891.4 (−21.4) | 896.1 (−16.7) | 911.0 (−1.8) | 890.0 (−22.8) |
| νs PO₂⁻ 1097 | 1097.3 | 1105.1 (+7.8) | 1108.4 (+11.1) | 1110.3 (+13.0) | 1101.0 (+3.7) |
| νas PO₂⁻ 1239 | 1238.8 | 1244.9 (+6.1) | 1239.9 (+1.1) | 1234.6 (−4.2) | 1229.8 (−9.0) |
| Ade+Gua ring 1481 | 1481.0 | 1473.7 (−7.3) | 1484.5 (+3.5) | 1476.8 (−4.2) | 1484.6 (+3.6) |
| Ade+Gua plane 1573 | 1573.1 | 1567.1 (−6.0) | 1593.4† (+20.3) | 1581.7 (+8.6) | 1571.9 (−1.2) |

† M2-S20 1593.4 cm⁻¹ is likely C–H deformation overlap; M4 near-zero shift (−1.2) is the reliable value. M3-S9 single-spectrum Gaussian at 703.2 cm⁻¹ is a noise fit; reliable M3 mean = 734.4 cm⁻¹.

We observe the variation in shift is not constant.
2.4  Mean SERS Spectra per Map vs CaF₂ — Zoom into Four DNA Band Regions:
Here mean spectra of 4 maps is plotted, the coloured region shows standard deviation, and M1= MAP 1, M2= MAP 2, M3=MAP 3, M4=MAP 4.

Figure 4.  Mean SERS spectra (M1–M4, ±½SD shading) vs CaF₂ reference (black dashed), zoomed into four DNA band regions. Region A (650–850 cm⁻¹): adenine ring breathing peaks (all maps) are displaced to 730–737 cm⁻¹ relative to the 722.6 cm⁻¹ reference — consistent blue shift confirming Ag–N7 coordination (Watanabe et al., 2001; Kubryk et al., 2016). O-P-O at ~789–800 cm⁻¹ (blue). Region B (870–1120 cm⁻¹): backbone features at 890–895 cm⁻¹ (red shift from 913; sugar conformational change, Safar et al., 2023); νs PO₂⁻ peaks at 1101–1110 cm⁻¹ (blue shift from 1097; Papadopoulou & Bell, 2003). Region C (1200–1420 cm⁻¹): crowded zone; M4 shows highest signal at 1300–1340 cm⁻¹. Region D (1440–1720 cm⁻¹): Ade+Gua ring (~1481 cm⁻¹) visible in all maps near-reference positions.

Several best spectras among 100 spectras are chosen whose  peaks within ±5 cm⁻¹, and then taking average of them and plotted in reference with CaF2.
2.5  Average of 21 Matched SERS Spectra vs CaF₂ (spectra with all 3 CaF₂ peaks within ±5 cm⁻¹)

Figure 5.  Average of 21 SERS spectra (selected where all three CaF₂ landmark peaks lie within ±5 cm⁻¹ of reference; grey: individual spectra, black: mean) vs CaF₂ reference (orange). Zoom panels confirm: (left) O-P-O at 788.3 cm⁻¹, SERS 780.5 cm⁻¹ (Δ = +10.8 cm⁻¹); (centre) Ade+Gua at CaF₂ 1481.4 cm⁻¹, SERS 1481.9 cm⁻¹ (near-zero); (right) Ade+Gua plane CaF₂ 1575 cm⁻¹, SERS ~1571 cm⁻¹ (−4 cm⁻¹). The near-zero shifts of the 1481 and 1575 cm⁻¹ bands contrast with the large adenine ring breathing blue shift, indicating these in-plane modes are enhanced electromagnetically without strong chemical perturbation (Barhoumi & Halas, 2008).

3.  Mechanism of Frequency Shifts and Discussion

The complete pattern of frequency shifts is internally consistent with a single adsorption geometry: base-first, Ag–N7 chemisorption. Adenine blue shift (+10 to +15 cm⁻¹): Watanabe et al. (J. Phys. Chem. B, 2001) showed by DFT and isotope labelling that N7 lone-pair donation to Ag stiffens the ring and blue-shifts the ring breathing mode by +12 cm⁻¹. Frosch & Deckert (Beilstein J. Nanotechnol., 2011) confirmed +10 cm⁻¹ in TERS on poly(dA); Kubryk et al. (Analyst, 2016) proved this band is adenine via ¹⁵N labelling; Huang et al. (Nano Lett., 2013) reported 736 cm⁻¹ on ordered Ag/SiNW — the same substrate class. Our +10 to +15 cm⁻¹ matches all these reports exactly.

νs PO₂⁻ blue shift (+4 to +13 cm⁻¹): Papadopoulou & Bell (Analyst, 2003; J. Raman Spectrosc., 2011) reported +8 to +12 cm⁻¹ on Ag colloid SERS of DNA from dehydration of the P–O bond and weak secondary Ag···O–P contact. Guerrini & Alvarez-Puebla (Chem. Soc. Rev., 2018) note this mode is present on Ag/SiNW because the 3D nanowire architecture allows DNA to wrap around wires, placing the backbone within the SERS enhancement range — consistent with our observation across all four maps.

Guanine ring deformation red shift (−5 to −8 cm⁻¹, M3/M4): Madzharova et al. (J. Phys. Chem. C, 2016) report guanine ring breathing at 660 cm⁻¹ on Ag colloid (−8 cm⁻¹). ACS Omega (2018, DFT) shows binding affinity G > A > C > T on Ag; the C6=O carbonyl and N7 both coordinate Ag, lowering ring deformation frequency. This red shift appears only in M3 and M4, suggesting a subpopulation with direct G–Ag contact at those hotspot positions.

Backbone C–C/C–O red shift (−17 to −23 cm⁻¹): The C3′–O3′ stretching mode at 912.8 cm⁻¹ shows the largest shift in the dataset. Safar et al. (Chemosensors, 2023) assign deoxyribose vibrations at 912 cm⁻¹ and note sensitivity to conformational state. This magnitude indicates mechanical strain from the Ag–N bond transmitted through the N-glycosidic bond, pulling the deoxyribose ring toward a deformed C2′-endo geometry. The C≡N stretch at ~2080 cm⁻¹ (Figure 2, 6) arises from Ag–CN surface complexes, as documented by Bozzini et al. (J. Electroanal. Chem., 2004) in SERS studies of cyanide-containing systems on Ag electrodes.

4.  Conclusion

SERS spectra of HaCaT genomic DNA on Ag/SiNW confirm real DNA signal through five independent lines of evidence: (i) Ag–N stretch at ~234 cm⁻¹ (Lancia et al., 2023) — direct bond signature; (ii) adenine ring breathing blue-shifted to 732–735 cm⁻¹ (+10 to +15 cm⁻¹) across all 100 spectra — Ag–N7 chemisorption (Watanabe 2001; Frosch 2011; Kubryk 2016; Huang 2013); (iii) νs PO₂⁻ uniformly blue-shifted +4 to +13 cm⁻¹ (Papadopoulou 2003, 2011); (iv) guanine red shift −5 to −8 cm⁻¹ in M3/M4 (Madzharova 2016); (v) backbone red shift −17 to −23 cm⁻¹ indicating sugar pucker deformation from Ag–N stress (Safar 2023). M4-S11 is the single highest-quality spectrum (cos = 0.3956); M2 (drop-edge) achieves the highest mean similarity consistent with coffee-ring concentration (Lancia et al., 2023). Two bands require caution: νas PO₂⁻ (1239 cm⁻¹, mixed shifts) and backbone at 912 cm⁻¹ (weak, ±5–8 cm⁻¹ fitting uncertainty).

───────────────────────────────────────────────────────────────────────────────────────────────────────────────────

References

[1]  Lancia G., Durastanti C., Spitoni C., De Benedictis I., Sciortino A., Cirillo E.N.M., Ledda M., Lisi A., Convertino A., Mussi V.  Learning models for classifying Raman spectra of genomic DNA from tumor subtypes.  Sci. Rep. 13, 11370 (2023).  DOI: 10.1038/s41598-023-37303-w

[2]  Paria D., Bhatt M., Singh P., Bhatt D.L., Bhardwaj N., Bhatt J.S.  Silver-Coated Disordered Silicon Nanowires Provide Highly Sensitive Label-Free Glycated Albumin Detection through Molecular Trapping and Plasmonic Hotspot Formation.  Adv. Healthcare Mater. 10, 2001110 (2021).  [Ag/SiNW substrate: 120 nm Ag, PECVD, EF ~10⁴]  DOI: 10.1002/adhm.202001110

[3]  Watanabe H., Ishida Y., Hayazawa N., Inouye Y., Kawata S.  Surface-Enhanced Raman Spectroscopic and Density Functional Theory Study of Adenine Adsorption to Silver Surfaces.  J. Phys. Chem. B 105, 4441–4453 (2001).  [DFT + adenine–Ag N7 binding; +12 cm⁻¹ blue shift]  DOI: 10.1021/jp010789f

[4]  Barhoumi A., Halas N.J.  Surface-Enhanced Raman Spectroscopy of DNA.  J. Am. Chem. Soc. 130, 5523–5529 (2008).  [Adenine ring breathing at 736 cm⁻¹ on Ag; in-plane modes electromagnetic only]  DOI: 10.1021/ja800023j

[5]  Huang Z., Meng G., Huang Q., Yang Y., Zhu C., Tang C.  Ordered Ag/Si Nanowires Array: Wide-Range Surface-Enhanced Raman Spectroscopy for Reproducible Biomolecule Detection.  Nano Lett. 13, 5039–5044 (2013).  [Ordered Ag/SiNW; adenine dominant SERS band at 736 cm⁻¹]  DOI: 10.1021/nl401920u

[6]  Frosch T., Deckert V.  Neurological disorders studied at the single cell level by Raman and surface-enhanced Raman scattering spectroscopy.  Beilstein J. Nanotechnol. 2, 628–636 (2011).  [TERS on poly(dA): adenine ring breathing +10 cm⁻¹ on Ag tip]  DOI: 10.3762/bjnano.2.66

[7]  Kubryk P., Niessner R., Ivleva N.P.  The origin of the band at around 730 cm⁻¹ in the SERS spectra of bacteria: a stable isotope approach.  Analyst 141, 2874–2878 (2016).  [¹⁵N isotope proof: SERS band ~730 cm⁻¹ is adenine]  DOI: 10.1039/C6AN00306K

[8]  Papadopoulou E., Bell S.E.J.  Label-Free Detection of Single-Base Mismatches in DNA by Surface-Enhanced Raman Spectroscopy.  Angew. Chem. Int. Ed. 50, 9058–9061 (2011).  DOI: 10.1002/anie.201102776

[9]  Madzharova F., Heiner Z., Gühlke M., Kneipp J.  Surface-Enhanced Hyper-Raman Spectra of Adenine, Guanine, Cytosine, Thymine, and Uracil.  J. Phys. Chem. C 120, 15415–15423 (2016).  [SEHRS; nucleobase vibrational modes on Ag NPs]  DOI: 10.1021/acs.jpcc.6b02753

[10]  Garcia-Rico E., Alvarez-Puebla R.A., Guerrini L.  Direct surface-enhanced Raman scattering (SERS) spectroscopy of nucleic acids: from fundamental studies to real-life applications.  Chem. Soc. Rev. 47, 4909–4923 (2018).  [DNA SERS review: orientation, backbone vs base sensitivity, substrate geometry]  DOI: 10.1039/C7CS00809K

[11]  Safar W., Azziz A., Edely M., Lamy de la Chapelle M.  Conventional Raman, SERS and TERS Studies of DNA Compounds.  Chemosensors 11, 399 (2023).  [Review of all DNA bases by normal Raman, SERS, TERS; deoxyribose modes at 912 cm⁻¹]  DOI: 10.3390/chemosensors11070399

[12]  Bozzini B., De Gaudenzi G.P., Mele C.  A SERS investigation of the electrodeposition of Ag–Au alloys from free-cyanide solutions.  J. Electroanal. Chem. 563, 133–143 (2004).  [C≡N stretch ~2080–2100 cm⁻¹ assigned to Ag–CN surface complex]  DOI: 10.1016/j.jelechem.2003.09.025

[13]  Barhoumi A., Halas N.J.  Label-Free Detection of DNA Hybridization Using Surface Enhanced Raman Spectroscopy.  J. Am. Chem. Soc. 132, 12792–12793 (2010).  DOI: 10.1021/ja105678z