# SERS Raman Map Analysis — DNA HaCaT on Ag/SiNW

4 Maps  |  532 nm  |  50XLF  |  0.5s × 4 acc  |  BC200  |  25% laser  |  5 µL drop  |  20 ng/µL

# 1. Acquisition Parameters

| Parameter | Value |
| --- | --- |
| Maps | M1 (drop center), M2 (drop edge), M3 (drop center), M4 (drop center) |
| Excitation | 532 nm |
| Objective | 50X LF |
| Exposure | 0.5 s x 4 accumulations |
| Laser power | 25% |
| Filter | BC200 |
| Spectra per map | 25 (5x5 grid) |
| Wavenumber range | ~201-3200 cm-1 ¦ Analysis window: 400-1800 cm-1 |
| Sample | DNA HaCaT, 20 ng/uL, 5 uL drop, dried before measurement |

# 2. Universal Substrate Peak — Si at 520 cm-1

The peak at 520-521 cm-1 appears in EVERY spectrum across ALL 4 maps without exception. This is the crystalline silicon peak from the SiNW substrate. It is the internal calibration reference. Its consistent presence confirms the substrate is intact.

# 3. Per-Map Summary

## M1 — Drop Center

| Property | Detail |
| --- | --- |
| Spatial grid | 0-16 um x 0-16 um |
| Intensity range | 4-210 counts (corrected) |
| Consistent peaks (all/most spectra) | 520 cm-1 (Si, all 25 spectra), 729-735 cm-1 (A ring breathing, 20/25 spectra) |
| Notable spectra | S24 @ (16,12): backbone cluster 723+803+905+959 cm-1 ¦ S10 @ (4,16): 770(53)+912(43) strong backbone ¦ S05 @ (0,16): 733+1331(33) Ade+Gua ¦ S17 @ (12,4): 733(35)+1341(33)+1614(73) richest fingerprint |
| Overall character | Moderate SERS. Adenine ring breathing (730-735 cm-1) is the most consistently enhanced band. DNA signal present in most spectra. Homogeneous compared to M2. |

## M2 — Drop Edge

| Property | Detail |
| --- | --- |
| Spatial grid | 0-16 um x 0-16 um |
| Intensity range | 4-92 counts (corrected) |
| Consistent peaks (all/most spectra) | 519-521 cm-1 (Si, all), 730-735 cm-1 (partial, ~12/25 spectra) |
| Notable spectra | S09 @ (4,12): HOTSPOT — 945(46)+1054(36)+1109(39)+1161(58)+1275(85)+1426(63)+1675(92) ¦ S23 @ (16,8): 799(58)+1169(78) strong O-P-O + Cyt C-H ¦ S07 @ (4,4): 1229(35)+1290(36) Cyt+Ade doublet ¦ S06/S14/S18/S20: almost no DNA signal beyond Si peak |
| Overall character | LOWEST average signal. Drop edge has less DNA. HIGH spatial heterogeneity — some hotspots and many dead zones. S09 is a genuine SERS hotspot at the dried ring edge. |

## M3 — Drop Center

| Property | Detail |
| --- | --- |
| Spatial grid | -25 to -10 um x -13 to +5 um |
| Intensity range | 4-491 counts (corrected) |
| Consistent peaks (all/most spectra) | 519-521 cm-1 (Si, all), 666 cm-1 (G ring def, majority), 729-736 cm-1 (A ring, majority) |
| Notable spectra | S20 @ (-13,+5): STRONGEST HOTSPOT of all maps: 914(303)+998(196)+1119(491)+1171(100)+1315(296)+1369(132)+1484(71) ¦ S21 @ (-10,-13): 666(118) strongest guanine ring deformation ¦ S18 @ (-13,-4): 741(30)+804(47) A ring + backbone ¦ S22 @ (-10,-8): 1277(56)+1325(22) strong Ade+Gua |
| Overall character | RICHEST DNA signal of all 4 maps. M3-S20 is the best SERS hotspot — all backbone, PO2- and nucleobase bands visible simultaneously. Most complete DNA fingerprint. |

## M4 — Drop Center

| Property | Detail |
| --- | --- |
| Spatial grid | -25 to -10 um x -13 to +5 um |
| Intensity range | 4-310 counts (corrected) |
| Consistent peaks (all/most spectra) | 519-523 cm-1 (Si, all), 733-736 cm-1 (A ring, majority), 1320-1340 cm-1 (Ade+Gua, majority) |
| Notable spectra | S09 @ (-21,0): max_I=310 — 957+1082+1106+1138+1148 backbone cluster ¦ S04 @ (-25,0): 960(152)+1325(44) very strong deoxyribose backbone ¦ S20 @ (-13,+5): 1148(80)+1346(101) strong PO2- and Ade+Gua ¦ S24 @ (-10,0): 848(50)+1200(44)+1328(67) |
| Overall character | Strong DNA signal, second only to M3. Same spatial grid as M3. Ade+Gua (1320-1340 cm-1) is the dominant nucleobase band throughout. |

# 4. DNA Peaks Present Across All 4 Maps

| cm-1 | Assignment | Occurrence | Notes |
| --- | --- | --- | --- |
| 520-521 | Si substrate | ALL spectra, all maps | Calibration reference, not DNA |
| 729-735 | Adenine ring breathing | Most spectra, ALL maps | Most reliably enhanced DNA band on Ag/SiNW |
| 779-797 | O-P-O / Thymine+Cytosine | Partial, all maps | Backbone marker |
| 909-914 | Backbone C-C/C-O | Most spectra, all maps | Deoxyribose backbone |
| 1058-1097 | Symmetric PO2- stretch | All maps | Phosphate backbone — I=491 in M3-S20 hotspot |
| 1160-1170 | Cytosine C-H / Thymine | All maps | Nucleobase fingerprint |
| 1315-1342 | Adenine + Guanine | Strong, all maps | Most prominent nucleobase band on SERS substrate |
| 1366-1369 | Thymine + Adenine | M3, M4 mainly | Clear in hotspot spectra only |
| 1480-1487 | Ade+Gua ring stretch | M2-S09, M3-S20, M4 | Matches CaF2 reference peak at 1483 cm-1 |
| 1560-1575 | Ade+Gua in-plane | M1, M2, M4 | Consistent with CaF2 reference |
| 1684-1691 | Guanine/Thymine C=O | M2-S09, M3-S21, M4-S06 | Carbonyl, nucleobase |

# 5. Which Map Spectra Match Each Other

Four groups identified by dominant spectral pattern:

## GROUP A — Backbone + PO2- dominated

DNA backbone is closest to Ag surface (backbone-down adsorption orientation). Strong bands: ~910-960 cm-1 (C-C/C-O), ~1097-1119 cm-1 (PO2-).

M3-S20 @ (-13,+5):  914, 998, 1119, 1315, 1369 — STRONGEST  (I_max = 491)

M4-S04 @ (-25,0):   960(152), 1146, 1248, 1325 — strong deoxyribose

M4-S09 @ (-21,0):   957, 1082, 1106, 1138, 1148 — backbone cluster

M1-S10 @ (4,16):    770, 912 — backbone pair

M2-S09 @ (4,12):    945, 1054, 1109, 1161 — backbone+PO2-

## GROUP B — Nucleobase rich (Ade+Gua dominant)

Purine nucleobases oriented toward Ag surface. Strong bands: 729-735 cm-1 (A ring), 1315-1342 cm-1 (Ade+Gua). Most common pattern across all 4 maps.

M1-S05 @ (0,16):    733, 1331 — A + Ade+Gua

M1-S07 @ (4,4):     735, 1330 — matches M1-S05 closely

M1-S17 @ (12,4):    733(35), 1341(33) — richest M1 spectrum

M2-S07 @ (4,4):     729, 1229, 1290 — Cyt+Ade doublet

M3-S19 @ (-13,0):   740, 1317, 1335 — A+G doublet

M3-S22 @ (-10,-8):  733, 1277, 1325 — A+G+PO2-

M4-S03 @ (-25,-4):  733, 1274, 1328 — A ring + Ade+Gua

M4-S08 @ (-21,-4):  733, 1293, 1335 — A+G doublet

M4-S15 @ (-17,+5):  1325 dominant

M4-S24 @ (-10,0):   738, 1200, 1267, 1328

## GROUP C — Full fingerprint (backbone + nucleobase both present)

Most information-rich spectra. Both PO2- and nucleobase bands visible — tilted DNA adsorption or mixture of orientations at a hotspot junction.

M3-S20 @ (-13,+5):   772, 914, 1119, 1315, 1369, 1484 — MOST COMPLETE

M2-S09 @ (4,12):     945, 1054, 1109, 1161, 1275, 1426, 1564, 1675 — full fingerprint

M3-S21 @ (-10,-13):  666(118), 1190, 1245, 1344, 1691 — G ring + Ade+Gua + C=O

M1-S15 @ (8,16):     736, 1012, 1143, 1190, 1243 — PO2- visible

M4-S20 @ (-13,+5):   1148(80), 1346(101) — strong PO2- + Ade+Gua

## GROUP D — Weak / Si background only

Essentially no DNA signal. Positions where dried DNA film is sparse or no plasmonic hotspot is present under the laser spot.

M2-S06 @ (4,0):    only 519, 735, 1327 detectable

M2-S14 @ (8,12):   only 519, 729 detectable

M2-S18 @ (12,8):   only 519, 787 detectable

M2-S20 @ (12,16):  only Si peak at 517 cm-1

M1-S01 @ (0,0):    weak broad features, no clear DNA peaks

# 6. M3 vs M4 — Same Spatial Grid Comparison

M3 and M4 share the same spatial coordinates (-25 to -10 um x -13 to +5 um). They measured the same region — either two separate drops or two repeat measurements.

Both maps show adenine ring breathing at 729-736 cm-1 consistently.

Both show Ade+Gua at 1315-1342 cm-1 as the dominant nucleobase band.

M3-S20 and M4-S04/S09 are at similar coordinates and both show hotspot-level intensity — confirming a persistent plasmonic hotspot at that spatial location.

M3 shows higher maximum signal (I=491) vs M4 (I=310) — possibly different hotspot coupling efficiency or slightly different DNA film thickness.

Cosine similarity between best-matched M3 and M4 spectra = 0.72 (moderate).

# 7. Comparison to CaF2 Reference Spectrum

CaF2 reference: 10s x 4 acc, 100X, max DNA signal ~137 counts above baseline.

| CaF2 Reference (cm-1) | Ag/SiNW Maps (cm-1) | Match |
| --- | --- | --- |
| 724 (A ring breathing) | 729-735, all maps | Confirmed — most enhanced band |
| 782 (O-P-O) | 779-797, partial | Present, weaker relative to nucleobase |
| 1097 (vs PO2-) | 1097-1119, all maps | Strongly enhanced in M3-S20 (I=491) |
| 1242 (vas PO2-) | 1229-1251, partial | Present, merged with backbone region |
| 1295-1326 (Ade+Gua) | 1290-1342, all maps | MOST ENHANCED — dominant in M3, M4 |
| 1367 (Thy+Ade) | 1355-1369, M3 and M4 | Visible in hotspot spectra |
| 1483 (Ade+Gua ring) | 1478-1487, M3-S20 and M2-S09 | Present in strongest spectra |
| 1574 (in-plane) | 1560-1591, M1, M2, M4 | Confirmed |
| 1684 (C=O) | 1675-1691, M2, M3, M4 | Present in hotspot spectra |

# 8. Key Conclusions

The Si substrate peak at 520-521 cm-1 is universal — confirms substrate integrity in all 4 maps.

M3 (drop center) has the richest DNA SERS signal. The hotspot at S20 (-13,+5) gives I_max = 491 counts vs ~137 on CaF2 — a genuine SERS enhancement at that point.

M4 (drop center, same grid as M3) is highly consistent with M3 — confirms reproducibility.

M1 (drop center, different grid 0-16 um) shows moderate DNA signal throughout — adenine and purine bands are dominant.

M2 (drop edge) has the weakest and most heterogeneous signal. DNA concentration is lower at the ring edge. Localized hotspots (S09, S23) still present.

The dominant enhanced DNA band on Ag/SiNW is Ade+Gua at 1315-1342 cm-1 (shifted ~15-20 cm-1 red vs CaF2 reference), suggesting direct nucleobase-Ag interaction.

All 9 major DNA Raman bands from the CaF2 reference are confirmed across the SERS maps.

Best single spectrum for DNA characterisation: M3-S20 @ (-13,+5 um) — shows backbone (914), PO2- (1119), and nucleobase (1315, 1369, 1484) simultaneously.