PEER REVIEW REPORT

Materials Chemistry and Physics  |  Elsevier

Manuscript No.  MATCHEMPHYSD2604411

| Title | Efficient Surface Enhanced Raman Scattering on Graphene Coated Cu Nanowires Prepared by Low Temperature Chemical Vapor Deposition |
| --- | --- |
| Authors | Van Tan Tran, An Bang Ngac, Nguyen Hai Pham, Viet Tuyen Nguyen, Van Chuc Nguyen, Trong Tam Nguyen, Bui Nguyen Quoc Trinh, The Nam Dinh, Thi Ha Tran* |
| Institution | Vietnam National University Hanoi; Vietnam Academy of Science and Technology; Vietnam Maritime University; Vietnam Japan University; Hanoi University of Mining and Geology |
| Date | 21 June 2026 |

1.  OVERALL ASSESSMENT

This manuscript describes fabrication of Cu/G nanowire SERS substrates via thermal oxidation, H2 reduction at 400 degrees C, and low-temperature ethanol CVD. The best substrate achieves LOD = 5.69x10^-11 M and EF = 6.1x10^6 for methylene blue, with 90-day stability. The fabrication concept is sound; however, the manuscript contains critical deficiencies in EF reporting, FDTD modelling, graphene characterisation, and oxidation protection evidence that must be addressed before acceptance.

RECOMMENDATION:   Major Revision Required

2.  REVIEWER COMMENTS

Comment 1 — Enhancement Factor: Incomplete Reporting  [CRITICAL]

The EF value (6.1x10^6) is reported without the raw intensities I_SERS and I_RS, the Raman peak selected, or confirmation that acquisition conditions were identical for both spectra. The EF type must be identified as Analytical Enhancement Factor (AEF = (I_SERS/C_SERS) / (I_RS/C_RS), Le Ru & Etchegoin, Principles of SERS, Elsevier, 2009, Eq. 4.4), and the reference Raman spectrum of MB at 10^-4 M on silicon must be provided. Without these, the reported EF cannot be independently verified.

AEF formula (Le Ru & Etchegoin, Eq. 4.4):

ISERS / CSERSIRS / CRS  =  ISERSIRS  x  CRSCSERS  =  ISERSIRS  x  10- 410- 10  =  ISERSIRS  x  10
              6

Comment 2 — FDTD Model Inconsistent with Real Substrate  [MAJOR]

The FDTD simulation models an isolated 100 nm sphere, whereas the actual substrate is a network of 1D nanowires whose SERS hot spots arise at inter-wire nanogap junctions -- a fundamentally different geometry with different plasmon resonance conditions. Furthermore, the simulation presents |E|^2 maps, whereas SERS enhancement scales as |E/E_0|^4 (Moskovits, Rev. Mod. Phys. 57, 783, 1985). The simulation results cannot therefore justify the experimental wavelength selection or the measured EF.

Correct EM EF scaling (Moskovits, 1985):

EFEM  ~  
                  ( |E(r)| / |E0
                      | )4

Comment 3 — Graphene Quality Not Quantified  [MAJOR]

Figure 7 shows a prominent D band (1367 cm^-1) with a weak 2D band, indicating highly defective graphene. The I(D)/I(G) ratio is neither reported nor discussed. The authors must report this ratio, estimate the sp2 domain size via the Tuinstra-Koenig relation (J. Chem. Phys. 53, 1126, 1970), and discuss implications for both the charge-transfer enhancement mechanism and oxidation barrier effectiveness.

Tuinstra-Koenig domain size formula:

La  (nm)  =  (2.4 x 10
              - 10)  x  
                  lambda4  x  I(G)I(D)

Comment 4 — Oxidation Protection Evidence is Insufficient  [MAJOR]

The 90-day stability claim rests solely on the absence of CuO/Cu2O Raman peaks, which cannot detect sub-monolayer oxidation. XPS of the Cu 2p(3/2) peak (Cu0 at ~932.6 eV vs. Cu2+ at ~933.6 eV) before and after ageing is required. A control experiment with bare Cu nanowires stored under identical conditions is also mandatory; without it, the stability improvement cannot be causally attributed to graphene.

Comment 5 — LOD Calculation Not Shown  [MAJOR]

The LOD (5.69x10^-11 M) is stated without the calculation method. The IUPAC-standard formula LOD = 3sigma/S must be applied, where sigma is the standard deviation of the blank signal and S is the slope of the calibration curve from Figure 12b. The numerical values of sigma and S must be reported.

IUPAC LOD formula:

LOD  =  3 sigmaS

Comment 6 — Environmental Monitoring Claim Unsupported  [MODERATE]

All detection experiments use only methylene blue, a strongly SERS-active dye that binds preferentially to graphene via pi-pi stacking and is not a standard environmental pollutant. The claim of environmental monitoring applicability must be supported by testing at least one relevant non-dye analyte, or removed from the abstract and conclusions.

Comment 7 — Melting Point Depression Not Quantified  [MODERATE]

The authors invoke the Gibbs-Thomson effect to explain nanowire fragmentation above 400 degrees C but do not apply the Pawlow formula to estimate the actual melting point depression for 100 nm Cu nanowires. This estimate is needed to confirm that fragmentation is a solid-state Rayleigh instability process and not melting of nanoscale Cu.

Pawlow melting point depression formula:

Tm(nano)  =  Tm(bulk)  x  [ 1  -  4 gamma VmDeltaHf x rhol x d ]

Comment 8 — Reproducibility: RSD Not Reported  [MODERATE]

Figure 13 reports reproducibility only qualitatively. The Relative Standard Deviation (RSD = sigma/mu x 100%) across all mapping positions must be calculated and reported. The accepted benchmark is RSD < 15-20% (Ding et al., Nature Reviews Materials 1, 16021, 2016). The number of positions sampled must also be stated.

RSD formula:

RSD (%)  =  sigmamu  x  100

Comment 9 — CVD Temperature Range Incomplete  [MODERATE]

The optimal CVD result occurs at 400 degrees C, the lowest temperature tested. Temperatures below 400 degrees C (e.g., 350, 375 degrees C) must be explored to confirm this is a true optimum and not the lower boundary of an insufficiently explored parameter space.

Comment 10 — Graphene Deposition Not Confirmed Elementally  [MODERATE]

Figure 6b does not identify or quantify a carbon peak after CVD. The C Kalpha signal (~0.277 keV) must be labelled and the carbon atomic percentage reported. Given EDS's limited sensitivity for light elements, XPS of the C 1s peak (~284.6 eV) is strongly recommended to confirm graphene rather than amorphous carbon deposition.

3.  SUMMARY TABLE

| No. | Issue | Priority |
| --- | --- | --- |
| 1 | EF formula -- raw intensities, peak, and EF type not shown | CRITICAL |
| 2 | FDTD sphere model wrong geometry; ¦E¦^2 used instead of ¦E¦^4 | MAJOR |
| 3 | Graphene D/G ratio not reported; domain size not calculated | MAJOR |
| 4 | No XPS or control experiment to confirm oxidation protection | MAJOR |
| 5 | LOD formula (3sigma/S) and values of sigma and S not shown | MAJOR |
| 6 | Only MB tested; environmental monitoring claim unsupported | MODERATE |
| 7 | Melting point depression not quantified | MODERATE |
| 8 | RSD of SERS mapping not calculated | MODERATE |
| 9 | CVD temperature range too narrow | MODERATE |
| 10 | Carbon EDS/XPS evidence for graphene deposition absent | MODERATE |

4.  REFERENCES CITED IN THIS REVIEW

[R1] Le Ru, E.C. & Etchegoin, P.G. Principles of Surface-Enhanced Raman Spectroscopy. Elsevier, 2009. [AEF: Eq. 4.4, p. 187]

[R2] Moskovits, M. Surface-enhanced spectroscopy. Rev. Mod. Phys. 57, 783 (1985). [|E|^4 EM scaling]

[R3] Tuinstra, F. & Koenig, J.L. Raman spectrum of graphite. J. Chem. Phys. 53, 1126 (1970). [D/G ratio]

[R4] Ding, S.-Y. et al. Nanostructure-based SERS. Nature Rev. Mater. 1, 16021 (2016). [RSD benchmark]

[R5] Pawlow, P. Z. Phys. Chem. 65, 545 (1909). [Melting point depression]

Review prepared for manuscript MATCHEMPHYSD2604411  |  Materials Chemistry and Physics (Elsevier)