## Slide 1
ML-Raman Classification of Chromonic Liquid Crystals on Different Substrates
Sunset Yellow (SSY) on PDMS, Gr-PDMS, SiO₂/Si and Gr-SiO₂/Si · 80 Raman spectra (20/class) · λ = 473 nm · Python (scikit-learn)
What I did
1
Raw spectra
80 spectra, 450–1800 cm⁻¹
2
Preprocessing
Savitzky–Golay smoothing, scaling on training folds only
3
VIP selection
Top 1000–2200 variables
4
Models
PLS-DA and SVM-RBF
5
Validation
5-fold CV, external test, permutation test
Key results
47.5%
4-class accuracy (both models): spectra overlap strongly
75%
Binary PDMS vs SiO₂/Si, mixed external test (SVM-RBF)
90%
Binary, graphene-only external test (PLS-DA)
p = 0.001
Permutation test (999): signal is real, not chance
Conclusion: ML reveals substrate- and graphene-dependent self-organisation of SSY that is invisible by eye. The main discriminating axis is the substrate (PDMS vs SiO₂/Si), and the best classifier depends on the samples: SVM-RBF for mixed sets, PLS-DA for graphene-coated sets.